Mechanical behavior of polymer composites

MECH 422/MECH 6581

Mid term exam solution

February 13, 2012

Open book, Open notes

- Question 1: (20 marks)

The plate has fibers along the y direction, while it is constrained along the x direction. It is a unidirectional layer. If we label 1 as fiber direction, and direction 2 is perpendicular to the fiber direction, then direction 1 is the same as y direction and 2 is same as x direction. The governing equation can be written as:

Putting in the loading and boundary conditions, above equation becomes:

(1)

We now need to determine the different terms.

From the statement of the problem:

Note the coefficient of thermal expansion of the fiber is obtained  from chapter 1 for S glass.

For best fit with results obtained from finite element method,

(from Table 2.1)

For best fit with finite element results,

Substituting into the equation for shear modulus above, one gets:

From equation (1)

Strain in the thickness direction:

- Question 2 (20 marks)

Putting in the loading and boundary conditions, the above equation becomes:

(2)

From equation (2)

Strain in thickness direction:

Angle at lower left hand corner increases by 0.0094 degrees.

Question 3: (20 marks)