## Slide 1
By
Ahmad O. Mostafa
Experimental Investigation of the Phase Equilibria in the
Mg-Mn-{Ce, Nd} and Ce-Mg-Zn Ternary Systems and Diffusivity Measurements of the Mg-{Ce, Nd, Zn}
and Zn-{Ce, Nd} Binary Systems
Supervisor
Dr. Mamoun Medraj
Doctoral Thesis Defense Presentation
May 20th , 2014
Mechanical Engineering
at
Concordia University
Montreal, Quebec, Canada
Notes: بسم الله الرحمن الرحيم

## Slide 2: Outlines
Introduction
Literature review
Methodology
Results and discussion
  Part 1: Ce-Mg-Zn ternary system
    Mg-Mn-{Ce, Nd} ternary systems
  Part 2: Binary diffusivity measurements of the Mg-Ce system
Conclusions
Contributions
Suggestions for future works

## Slide 3: Introduction
Distribution of greenhouse gas emissions by economic sector, Canada, 2012.
http://ec.gc.ca/indicateurs-indicators/default.asp?lang=en&n=F60DB708-1
The worldwide trend is towards more sustainable energy sources instead of the traditional fuel.
1- Innovate design for high performance vehicles.
2- Substitution of materials with lighter weight alternatives.
Mg
Notes: A breakdown of Canada’s emissions by economic sector shows the sources of Canada’s greenhouse gas (GHG) emissions in 2012. The emissions can be attributed to seven key areas of the economy
Promising

## Slide 4: Introduction
New Mg alloy systems provide promising opportunities for improved properties and performance suitable for demanding applications.
It is essential to understand the phase relationships resulting from these additions.
Mn
Zn
Improve corrosion resistance and mechanical properties at room temperature
Ce
Nd
Improve the mechanical properties at elevated temperatures
Alloying elements, added to Mg, improve its mechanical properties by solid-solution strengthening and/or by precipitation hardening.
Notes: Specific strength= strength/density
Drives us to the following objectives

## Slide 5
Experimental investigation of the phase equilibria in the:
  Mg-Mn-{Ce, Nd} systems at 450°C
  Ce-Mg-Zn system at 300°C
Objectives
Diffusivity measurements of the Mg-{Ce, Nd, Zn} and Zn-{Ce, Nd} binary systems.

## Slide 6
Literature
review

## Slide 7
Literature review
Kevorkov and Pekguleryuz, J. Alloy. Compnd. 2009, 478, 427-436.
350°C
300°C
Melnik et al., Magnievye Splavy. Mater.Vses. Soveshch. Issled., Razrab. Primen. Magnievyhk Splavov 1978, 95-99
Ce-Mg-Zn system
?
?
197°C
Pavlyuk et al., Intermetallics 2012, 20, 8-15.
197°C
M. Mezbahul-Islam et al. , Journal of Materials, (2014) Article ID: 704283
It is important to
Reveal the phase equilibrium in the Zn-rich corner
Verify the ternary compounds at 300°C
Investigate the unstudied regions

## Slide 8
Ce-Mg-Mn system
Literature review
Petrov et al., Baikov Institute of Metallurgy and Materials Science, 1 (1957) 144-147
Using thermal and metallographic methods
Zhang et al., Journal of Alloys and Compounds 482 (2009) 420–428
0.6 wt.% Mn
1.8 wt.% Mn
2.5 wt.% Mn
- Mg-rich corner only
- Few experimental data
- Predicted projection
Phase equilibrium
α-Mg+Mn
α-Mg+Mg9Ce
Mg9Ce=Mg12Ce
Using CALPHAD method

## Slide 9
Mg-Mn-Nd system
Literature review
Only one study was found in the literature
The study was limited to Mg-rich corner up to 4 wt.% Mn and 10 wt.% Nd.
The objective was to determine the solid solubility of Mn and Nd in Mg.
M. Drits et al, Journal of Inorganic Chemistry, 7 (1963) 2771-2777.
Because Mg-Mn-{Ce, Nd} systems are not completely studied, it is necessary to investigate them in the full composition range.
Phase equilibrium
α-Mg+Mn
α-Mg+Mg41Nd5

## Slide 10
Binary diffusivity
Literature review
S. Brennan et al., ICCMA, 2012, pp. 417-421
400°C
Xu et al., Journal of Materials Research, 16 (2001) 3287-3292
500°C
No diffusion information could be found about the Zn-{Ce, Nd} systems
The available coefficients of the Mg-{Nd, Zn} in the literature were found inaccurate due to missing phases.
M. Mezbahul-Islam et al. , Journal of Materials, (2014) Article ID: 704283
315°C
S. Brennan et al., Magnesium Technology 2012, John Wiley & Sons, Inc., 2012, pp. 323-327
It is necessary to provide accurate diffusion measurements.
Mg41Nd5?
MgNd?
Mg12Zn13?
315°C
500°C
400°C
315°C

## Slide 11: Methodology
Ce-Mg-Zn
Mg-Mn-Nd
Ce-Mg-Mn
Mg
Mn
Zn
Nd
Ce
Ce
Mg-Zn
Ce-Zn
Nd-Zn
Ce-Mg
Mg-Nd
Mg
Zn
Ce
Nd
Ce
Nd
Zn
Mg-Mn-{Ce, Nd} and Ce-Mg-Zn ternary systems
Mg-{Ce, Nd, Zn} and Zn-{Ce, Nd} binary systems
Binary
diffusion couples
Boltzmann-Matano
analysis
Ternary
diffusion couples
Key alloys
Binary interdiffusion
coefficients
Activation energies
Pre-exponential
factors
Isothermal
sections

## Slide 12
Phase diagram determination methods
Key alloys preparation
Diffusion couples prepared from pure metals and/or alloys
  End-members were selected to cover large area of the studied system
  Polishing up to 1μm diamond suspension → clamping → annealing
Alloys were prepared in arc-melting and/or induction-melting furnaces
Chemical composition→ ICP-OEM and/or EDS
Diffusion couples preparation
Induction melting furnace
Analysis
XRD (Phase identification and relative phase amount)
WDS/EDS (Phase composition)
SEM (microstructural studies)
Methodology
Notes: Talk about different annealing time intervals.

## Slide 13
Binary diffusivity measurements
Y. Du et al., Atomic Mobilities and Diffusivities in Al alloys, Sci. China Tech. Sci., 55 (2012) 1-23.
Ď(c): interdiffusivity at the composition C (cm2/sec)
t: annealing time (sec)
dc/dx : slope at the composition C (at.%/cm),
x: layer thickness (cm).
Calculating the coefficients directly from the composition profile
The magnitude of the diffusion coefficient (D) is indicative of the rate which atoms diffuse.
Methodology
Q: the activation energy for diffusion (J/mole)
D: temperature-independent pre-exponential (cm2/sec)
R: the gas constant (8.31 J/mole.K)
T : absolute temperature (K)
Qd and Do can be calculated using diffusion couples annealed at different temperatures and Arrhenius plot.
The slope is -Qd/2.3R, and
the intersection with y axis is logDo .
logD vs. 1/T
Notes: This is another option for an Overview slides using transitions.

## Slide 14
Results
And
discussion
Ce-Mg-Zn
Mg-Mn-Nd
Ce-Mg-Mn
Mg
Mn
Zn
Nd
Ce
Ce
Phase equilibria of the Ce-Mg-Zn at 300°C
Results and discussion
Results part 1:
(1) Diffusion multiple
(3) Diffusion couples
(28) Key alloys
Tie-line interpolation technique

## Slide 15
Diffusion multiple- Ce/Mg/Zn
Annealing temp.: 300°C
Annealing time: 21 days
Line-scan
Ce
Zn
Mg
1
2
3
4
5
2
6
7
8
9
X
Mg-Zn
Ce-Mg
Ce-Zn
Diffusion path
Composition profile
Results: Part 1
Notes: Diffusivity of different elements

## Slide 16
Diffusion couple #1- Mg+CeMg12/Zn
Annealing temp.: 300°C
Annealing time: 21 days
CeMg12
Mg+CeMg12
Zn
CeMg12
Mg+CeMg12
Zn
Mg2Zn11
Mg2Zn11+(Ce2Zn17)
MgZn2+(Ce2Zn17)
MgZn2
τ6
τ5
CeMg12
Ce(Mg,Zn)12
τ5
τ2
MgZn2
Mg2Zn3
Original interface
Remarks
Four ternary compounds were found (τ2, τ5, τ6 and τ8)
Mg was found in equilibrium with:
  CeMg12
  (CeMg12)
  τ2
  τ8
  Mg12Zn13
Results: Part 1
Mg
τ8
Notes: Single phase layer and two-phase layer

## Slide 17
A
B
C
E
D
Mg
A
B
C
E
D
Ce
Zn
EDS elemental mapping
Diffusion couple #1- Mg+CeMg12/Zn
A
B
C
E
D
A
B
C
E
D
Almost constant at ~8 at.%
Results: Part 1

## Slide 18
Diffusion couple #1- Mg+CeMg12/Zn
Annealing temp.: 300°C
Annealing time: 21 days
Phase relationships analysis
WDS line-scans/spots
EDS elemental maps
Phase equilibrium
Results: Part 1

## Slide 19
Diffusion couples #2 and 3
Phase equilibria representation
Zn/(CeMg3+CeMg) diffusion couple
Annealed at 300°C for 21 days
CeMg3+CeMg
Zn
Ce/(Mg+Mg12Zn13) diffusion couple
Annealed at 300°C for 40 days
(Mg)Zn
Ce
CeZn
CeZn2
τ3
τ7
τ5
τ2
Three ternary compounds were found (τ3, τ5 and τ6)
Four ternary compounds were found (τ2, τ3, τ5 and τ7)
Results: Part 1

## Slide 20
Combined diffusion multiple/couples results
Phase equilibrium obtained from a diffusion multiple and three diffusion couples at 300°C
Melnik et al., Magnievye Splavy. Mater.Vses. Soveshch. Issled., Razrab. Primen. Magnievyhk Splavov 1978, 95-99
Results: Part 1
Key alloys
Notes: I am proud

## Slide 21
Key alloys
To confirm the obtained phase relationships
To verify the ternary compounds
To investigate the unstudied regions
To determine the solid solubilities
28 key alloys
Annealing
For ≥ 30 days
WDS and XRD
1
2
12
Results: Part 1

## Slide 22
Results: Part 1
Alloys with three-phase equilib.
WDS and XRD analysis are consistent
1
2
12
(Ce2Zn17)
Zn
Mg2Zn11
Sample #1
Mg2Zn11
MgZn2
(Ce2Zn17)
Sample #2
τ3
Sample #12
(CeZn2)
Ce(Mg,Zn)
Alloys with two-phase equilib.
(Ce3Zn22)
(Ce2Zn17)
Sample #3
Sample #10
Ce(Mg,Zn)
Ce(Mg,Zn)3
MgZn2
(Ce2Zn17)
Sample #23
Two-phase alloys give tie-lines

## Slide 23
Boundary tie-lines
Interior tie-lines
Interpolation of tie-lines on a ternary system
A
B
C
D
Results: Part 1

## Slide 24
Ce-Mg-Zn isotherm at 300°C
(1) Diffusion multiple
(3) Diffusion couples
(28) Key alloys
Tie-line interpolation technique
Published as: Ahmad Mostafa and Mamoun Medraj , Phase equilibria of the Ce-Mg-Zn ternary system at 300°C, Metals, accepted on May 15, 2014.
Results: Part 1
Remarks
Isothermal section constructed in the full composition range
Eight ternary compounds were found at 300°C

## Slide 25
Mg-Mn-{Ce,Nd} and Ce-Mg-Zn ternary systems
Ce-Mg-Mn system at 450°C
Results: Part 1
Mg-Mn-Nd system at 450°C
Diffusion couples
Key alloys
WDS and XRD
Remarks
Isothermal sections were constructed in the full composition range at 450°C
No ternary compound was found
Ternary solid solubilities were determined
Mn was found in equilibrium with most of the phases in both systems
Mg-Mn-Nd (450°C)
Ce-Mg-Mn (450°C)
Mg
Mn
Nd
Ce
Ce-Mg-Zn (300°C)
Zn
Ce
Degree of complexity
Published as: Ahmad Mostafa and Mamoun Medraj , Experimental investigation of the Ce-Mg-Mn isothermal section at 723K (450°C) via diffusion couples technique, Metallurgical and Materials Transactions A, Vol. 45 (7), pp. 3144-3160, 2014.
Published as: Ahmad Mostafa and Mamoun Medraj Experimental investigation of the Mg-Mn-Nd isothermal section at 450°C, Journal of Alloys and Compounds; Vol. 608, pp. 247-257, 2014.
Ce-Mg-Zn system at 300°C
CHAPTER 3: Mg-Mn-Nd (450°C)
CHAPTER 2: Ce-Mg-Mn (450°C)
CHAPTER 4: Ce-Mg-Zn (300°C)

## Slide 26
Published as: Ahmad Mostafa and Mamoun Medraj , On the atomic interdiffusion in Mg-{Ce, Nd, Zn} and Zn-{Ce, Nd} binary systems, Journal of Materials Research, submitted March, 2014.
Results and discussion
Mg-Zn
Ce-Zn
Nd-Zn
Mg-Ce
Mg-Nd
Mg
Zn
Ce
Nd
Ce
Nd
Zn
Mg-{Ce, Nd, Zn} and Zn-{Ce, Nd} binary systems
Results part 2:
Notes: Moving to diffusivity

## Slide 27
Mg-Ce binary system
Mg2Ce
490°C
400°C
450°C
Mg
Mg3Ce
Mg41Ce5
Mg12Ce
MgCe
Ce
400°C for 120hr
Mg
Mg41Ce5
Mg12Ce
Mg3Ce
MgCe
Ce
490°C for 48hr
Ce
Mg
MgCe
Mg3Ce
Mg41Ce5
450°C for 96hr
Mg12Ce
A. Nayeb-Hashemi and J. Clark: ASM Handbook, Volume 03—Alloy Phase Diagrams, ASM International, Materials Park, OH, 1992
Diffusivity measurements
Results: Part 2
Line-scan
Y. Du et al., Atomic Mobilities and Diffusivities in Al alloys, Sci. China Tech. Sci., 55 (2012) 1-23.
Co
xo
System | Intermetallic interface | Co | 400°C |  | 450°C |  | 490°C | 
 |  | Mg (at.%) | xo (µm) | Do(C) (cm2/s) | xo (µm) | Do(C) (cm2/s) | xo (µm) | Do(C) (cm2/s)
Mg-Ce | Ce/MgCe | 25 | 9.7 | 1.8×10-13 | 4.1 | 3.5×10-13 | 9.8 | 6.0×10-13
 | MgCe/Mg3Ce | 62.5 | 12.6 | 8.7×10-14 | 9.2 | 1.6×10-13 | 16.2 | 3.2×10-13
 | Mg3Ce/Mg41Ce5 | 82 | 22.0 | 1.6×10-13 | 19.5 | 3.2×10-13 | 33.5 | 5.6×10-13
 | Mg41Ce5/Mg12Ce | 90.7 | 60.8 | 1.1×10-13 | 89.6 | 2.3×10-13 | 133.3 | 4.2×10-13
 | Mg12Ce/Mg | 96 | 84.4 | 2.1×10-13 | 118.0 | 4.8×10-13 | 150.9 | 7.3×10-13
logD vs. 1/T
The slope is -Qd/2.3R, and
the intersection with y axis is logDo .
Activation energy and pre-exponential factor
System | Intermetallic interface | Qd (kJ/mole) | Do (cm2/s)
Mg-Ce | Ce/MgCe | 56.1 | 4.2×10-9
 | MgCe/Mg3Ce | 61.9 | 5.4×10-9
 | Mg3Ce/Mg41Ce5 | 58.9 | 5.6×10-9
 | Mg41Ce5/Mg12Ce | 61.3 | 6.6×10-9
 | Mg12Ce/Mg | 58.1 | 7.3×10-9
ΔlogD
Δ(1/T)
Mg
Notes: We understood the shortcoming of the literature and we could discover all the expected phases
Results were comparable to the literature

## Slide 28: Conclusions
Conclusions
Diffusion couples combined with equilibrated key alloys are used to investigate the phase equilibria of the studied systems.
The isothermal sections of the Mg-Mn-{Ce, Nd} are established at 450°C and of the Ce-Mg-Zn is established at 300°C in the full composition range.
Eight ternary compounds are observed in the Ce-Mg-Zn system at 300°C.
The binary interdiffusion coefficients of the Mg-{Ce, Nd, Zn} and Zn-{Ce, Nd} systems are measured.
The activation energies and pre-exponential factors of the growth of the Mg-{Ce, Nd, Zn} compounds are also calculated.

## Slide 29: Contributions
Ahmad Mostafa and Mamoun Medraj, “Phase equilibria of the Mg-Nd-Zn ternary system at 300°C by means of diffusion couples and key alloys techniques,” (In preparation).
A. O. Mostafa, A. E. Gheribi, D. Kevorkov, M. Mezbahul-Islam, and M. Medraj, “Experimental Investigation and Thermodynamic Modeling of Mn-Nd Phase Diagram,” CALPHAD, 2013, Vol. 42, pp. 27-37.
Tian Wang, Dmytro Kevorkov, Ahmad Mostafa, and Mamoun Medraj “Experimental investigation of the phase equilibria in the Al-Mn-Zn system at 400°C,” Journal of Materials, submitted April, 2014.
Md. Mezbahul-Islam, Ahmad Mostafa, and Mamoun Medraj, "Essential Magnesium Alloys Binary Phase Diagrams and their Thermochemical Data", Journal of Materials, Volume 2014, Article ID 704283.
Md. I. Khan, A. Mostafa, M. Aljarrah, E. Essadiqi and M. Medraj, "Influence of cooling rate on microsegregation behavior of magnesium alloys", Journal of Materials, Volume 2014, Article ID 657647, 18 pages.
Other journal publications

## Slide 30
Conference publications
“The Mg-Mn-Nd system: Experimental Investigation and Thermodynamic Modeling”, The 9th International Conference on Magnesium Alloys and their Applications, Vancouver, 2012, p.p. 245-250.
“Experimental Investigation of the Ce-Mg-Mn Isothermal Section at 450°C via Diffusion Couples and Key Alloys Techniques,” MIE-Concordia University, Montreal, April, 2014. Poster Presentation. PhD Seminar Award.
“Experimental investigation of the Mg-{Mn,Zn}-{Ce-Nd} ternary phase diagrams,” MagNET AGM2013, University of British Colombia, Vancouver. Oral presentation.
“The Assessment of Atomic Interdiffusion of the Mg-Mn-Nd Ternary System and its Constituent Binaries”, The 9th MagNET workshop at McGill University, Montreal, November, 2012. Poster Presentation.
“Isothermal Section of the Mg-Mn-Nd system at 450C: Experimental Investigation and Thermodynamic Modeling”, MagNET AGM, Waterloo, June 2012. Poster Presentation. Best Poster Award.
“Experimental Investigation and Thermodynamic Modeling of Mg-{Mn, Zn}-{Ce, Nd} Ternary systems”, MagNET AGM, Vancouver, June 2011.
Symposium records
Contributions

## Slide 31: Future works
Crystallographic studies of the newly discovered intermetallic compounds in the Ce-Mg-Zn at 300°C are essential.
Thermodynamic description is essential for establishing a self-consistent database of all ternary systems.
Liquidus projections are also essential for the thermodynamic description of the studied ternary systems. This can be achieved by the thermal analysis using DSC.
Diffusivity of the Mg-Mn-{Ce, Nd} and Ce-Mg-Zn ternary systems are important to be measured.

## Slide 32: Acknowledgements
Prof. Mamoun Medraj (thesis supervisor)
PhD committee members and examiners
Mr. Mazen Samara
Dr. Dmytro Kevorkov
Dr. Md. Mezbahul-Islam
TMG members
MagNET-NSERC (funding)
My family

## Slide 33
Thank you
Questions