## Slide 1: Experimental investigation of the Mg-{Mn, Zn}-{Ce, Nd} ternary phase diagrams
MagNET AGM
Vancouver, June 12-13, 2013
Presented by
Ahmad Mostafa
Supervisor
Dr. Mamoun Medraj

## Slide 2: Acknowledgement
NSERC MagNET
Dmytro Kevorkov – Research associate – Concordia University
Aimen Gheribi – Research fellow – École Polytechnique de Montréal
Pampa Ghosh – Research fellow – Concordia University
Md. Mezbahul-Islam – PhD candidate – Concordia University

## Slide 3: Outlines
Scope
Methodology
Results
Summary
Contributions

## Slide 4: Scope
Studying the interdiffusion coefficients of the binary and ternary species of the Mg-{Mn, Zn}-{Ce, Nd} systems using diffusion couple experiments and Boltzmann-Matano analysis.
The construction of the Mg-{Mn, Zn}-{Ce, Nd} ternary phase diagrams experimentally, by means of key alloys and diffusion couples, using DSC, XRD and SEM/EDS/WDS.

## Slide 5
Mg-{Mn, Zn}-{Ce, Nd} systems
Mg
Mn
Zn
Ce
Nd
Mg-Zn
Mg-Mn
Ce-Mn
Ce-Zn
Nd-Zn
Nd-Mn
Ce-Mg
Mg-Nd
Ce-Mg-Zn
Mg-Mn-Nd
Mg-Nd-Zn
Ce-Mg-Mn
Literature
Data
Experimental
Investigation
Self-consistent Mg-{Mn, Zn}-{Ce, Nd} ternary phase diagrams
Binary and ternary diffusion coefficients database

## Slide 6
Methodology
Pure metals (Ce, Mg, Mn, Nd and Zn) were initially used
Alloying processes:
  Arc-melting furnace
  Induction-melting furnace
Key samples Preparation
Diffusion couples prepared from pure metals and/or alloys.
  Contacting surfaces polished up to 1μm diamond suspension
  End-members clamped together using stainless steel rings
Diffusion couples Preparation
XRD, WDS/EDS, SEM, DSC and ICP key experiments
Notes: Talk about the outcomes of each experiment. DSC, to detect the phase transformation and the liquidus temperatures. XRD, to know the relative amount of each phase.

## Slide 7
Methodology
Interdiffusion coefficient measurements
Y. Du et al., Atomic Mobilities and Diffusivities in Al alloys, Sci. China Tech. Sci., 55 (2012) 1-23.
: the flux of i atoms
Ď(c): is the interdiffusivity at the composition C (cm2/sec)
t: is the annealing time (sec)
dc/dx : is the slope at the composition C (at.%/cm),
x: is the layer thickness (cm).
…….…(1)
)dCi…………(2)
Boundary conditions
Notes: The phenomenon of diffusion can be demonstrated with the use of diffusion couple technique.

## Slide 8
Results
Mn-Nd binary phase diagram
Lattice parameters of Mn17Nd2
Mn23Nd6
Mn17Nd2
β-Mn
Mn23Nd6
Mn23Nd6
Mn17Nd2
Mn2Nd
Mn17Nd2
β-Mn

## Slide 9
Results
Mg-Mn-Nd ternary phase diagram
Diffusion couples experiments
450°C-for 20 days
(Nd)
Mg3Nd
Mn
Mg3Nd
Mg3Nd
Mg41Nd5
Mn23Nd6
Mn
450°C-for 9 days
(Nd)
Mn
Mg3Nd
MgNd
Mg41Nd5
Mg
Mn
Mn

## Slide 10
Results
Mg-Mn-Nd ternary phase diagram
Key alloys experiments
450°C-for 14 days
Mn
Mg3Nd
Mg41Nd5
Mn
Nd(Mg1-xMnx)
(Nd)Mg,Mn
450°C-for 14 days
Notes: Talk about the outcomes of each experiment. DSC, to detect the phase transformation and the liquidus temperatures. XRD, to know the relative amount of each phase.

## Slide 11
Results
Isothermal section of the Mg-Mn-Nd system at 450°C
By means of:
Key alloys and diffusion couples and using XRD, EPMA and metallography

## Slide 12
Results
490°C
450°C
400°C
Interdiffusion coefficients of Ce in Mg
400°C- 120h
450°C- 96h
490°C- 48h
MgCe
Mg3Ce
Mg41Ce5
Mg12Ce
H Okamoto, Ce-Mn (Cerium-Manganese), Journal of Phase Equilibria and Diffusion, 2008; 29: 381-2

## Slide 13
Results
Interdiffusion coefficients of Ce in Mg
 |  | Thickness (µm) |  | 
 | Temperature (°C) | 400 | 450 | 490
 | Time (h) | 120 | 96 | 48
Mg-Ce | MgCe | 3.5 | 5.9 | 8.7
 | Mg3Ce | 5.8 | 8.6 | 16.7
 | Mg41Ce5 | 39.7 | 71.5 | 101.4
 | Mg12Ce | 21.6 | 31.2 | 19.6
 | Total thickness | 70.6 | 117.2 | 145.4
Chart: 
| 0 | 48
490-48hrs | 0 | 145.7
450-96hrs | 0 | 117.2
400-120 hrs | 0 | 70.3
 | Intermetallic interface | 400°C |  | 450°C |  | 490°C | 
 |  | xo (µm) | (C) (cm2/S) | xo (µm) | (C) (cm2/S) | xo (µm) | (C) (cm2/S)
Mg-Ce | Ce/MgCe | 9.7 | 1.8×10-13 | 4.1 | 2.9×10-13 | 9.8 | 6.0×10-13
 | MgCe/Mg3Ce | 12.6 | 8.7×10-14 | 9.2 | 1.6×10-13 | 16.2 | 3.2×10-13
 | Mg3Ce/Mg41Ce5 | 22.0 | 1.6×10-13 | 19.5 | 3.6×10-13 | 33.5 | 5.6×10-13
 | Mg41Ce5/Mg12Ce | 60.8 | 1.1×10-13 | 89.6 | 2.3×10-13 | 133.3 | 4.2×10-13
 | Mg12Ce/Mg | 84.4 | 3.1×10-13 | 118.0 | 4.8×10-13 | 150.9 | 7.3×10-13
 | Intermetallic interface | 400°C |  | 450°C |  | 490°C | 
 |  | xo (µm) |  | xo (µm) |  | xo (µm) | 
Mg-Ce | Ce/MgCe | 9.7 | 1.8×10-13 | 4.1 | 2.9×10-13 | 9.8 | 6.0×10-13
 | MgCe/Mg3Ce | 12.6 | 8.7×10-14 | 9.2 | 1.6×10-13 | 16.2 | 3.2×10-13
 | Mg3Ce/Mg41Ce5 | 22.0 | 1.6×10-13 | 19.5 | 3.6×10-13 | 33.5 | 5.6×10-13
 | Mg41Ce5/Mg12Ce | 60.8 | 1.1×10-13 | 89.6 | 2.3×10-13 | 133.3 | 4.2×10-13
 | Mg12Ce/Mg | 84.4 | 3.1×10-13 | 118.0 | 4.8×10-13 | 150.9 | 7.3×10-13

## Slide 14
Results
Activation energies and pre-exponent factors
 | Intermetallic interface | Qd (kJ/mol) | o (cm2/S)
Mg-Ce | Ce/MgCe | 55.1 | 3.3×10-9
 | MgCe/Mg3Ce | 61.9 | 5.4×10-9
 | Mg3Ce/Mg41Ce5 | 58.9 | 6.4×10-9
 | Mg41Ce5/Mg12Ce | 61.3 | 6.6×10-9
 | Mg12Ce/Mg | 58.1 | 7.3×10-9
 | Intermetallic interface | Qd (kJ/mol) | 
Mg-Ce | Ce/MgCe | 55.1 | 3.3×10-9
 | MgCe/Mg3Ce | 61.9 | 5.4×10-9
 | Mg3Ce/Mg41Ce5 | 58.9 | 6.4×10-9
 | Mg41Ce5/Mg12Ce | 61.3 | 6.6×10-9
 | Mg12Ce/Mg | 58.1 | 7.3×10-9
Arrhenius relationship
1/T vs. logD
The slope represents –Qd/2.3R and the intersection with y axis represents the log Do value.

## Slide 15
Summary
The isothermal sections of the Mg-Mn-{Ce,Nd} ternary systems, at 450°C, were established by means of key alloys and diffusion couples.
The Mn-Nd binary phase diagram was constructed in the complete composition range using experimental work and first-principles calculations coupled with thermodynamic modeling.
The interdiffusion coefficients of Ce, Nd and Zn in Mg were determined using diffusion couple experiments and Boltzmann-Matano analysis.
Notes: Talk about the outcomes of each experiment. DSC, to detect the phase transformation and the liquidus temperatures. XRD, to know the relative amount of each phase.

## Slide 16
Contributions
A. Mostafa, A.E. Gheribi, D. Kevorkove, Md. Mezbahul-Islam, M. Medraj, “Experimental Investigation and First Principle Calculations Coupled with Thermodynamic Modeling of the Mn-Nd phase diagram”, CALPHAD, submitted, March 2013.
Journal papers
Conference proceedings
A. Mostafa, D. Kevorkove, A.E. Gheribi, M. Medraj, “The Mg-Mn-Nd system: Experimental Investigation and Thermodynamic Modeling”, The 9th International Conference on Magnesium Alloys and their Applications, Vancouver, 2012, p.p. 245-250.
P. Ghosh and M. Medraj, “Thermodynamic Calculation of the Mg-Mn-Zn and Mg-Mn-Ce Systems and Re-optimization of their Constitutive Binaries”, CALPHAD, Vol. 41, 89-107 (2013)
P. Ghosh, Md. Mezbahul-Islam and M. Medraj,"Critical assessment and thermodynamic modeling of Mg–Zn, Mg–Sn, Sn–Zn and Mg–Sn–Zn system", CALPHAD (Computer Coupling of Phase Diagrams and Thermochemistry), Vol. 36, 28-43 (2012).
Notes: Talk about the outcomes of each experiment. DSC, to detect the phase transformation and the liquidus temperatures. XRD, to know the relative amount of each phase.

## Slide 17: THANK YOU
MagNET AGM
Vancouver, June 12-13, 2013