## Slide 1: Hydrogen Storage Properties of Mg-Ni-H through Pressure Composition Isotherms Combined with Thermodynamic Calculations Guy-Joël Rocher
Master’s Thesis Defense Presentation
Supervisors: Dr. M. Medraj
Dr. H.D. Ng
December 6th , 2012
Thermodynamics of Materials Group
Department of Mechanical & Industrial Engineering
Concordia University

## Slide 2: Outline
Introduction
Motivation
Experimental Procedures
Results & Discussion
Concluding Remarks & Future Work

## Slide 3: 1. Introduction

## Slide 4: Environmental Concerns
Canada ranks 3rd in the world CO2 emissions per capita
16.33 metric tons/capita
Environment Canada, 2011
Environment Canada, 2011
Introduction
(Statistics Canada 2008)
Notes: Behind USA, Australia
Future trends : mining & oil

## Slide 5: Hydrogen Energy
What is Hydrogen Energy?
  2H2 + ½ O2 + 2e-  H2O
  H2 is an Energy Carrier
  Hydrogen = Electrification
Advantages
  Reduction in emission
  Energy efficiency increase
  Localized energy production
  Strengthen large scale electrical grid
Introduction
http://www.alternative-energy-news.info/technology/fuel-cells/
  H22H+ + 2e-
Notes: Fuel Cell Technology is mature
  Reduction of oil dependency

## Slide 6: Hydrogen Energy Barriers
Safety
Storage
Introduction
H2
(750bar)
Metal/Complex Hydride
Adsorption
Carbon
Chemical
Reactions
H2
(Liquid)
http://jksalescompany.com/ken/toyotayaris2012.html
Dr. Michael Swain, University of Miami, 2001
t = 3 sec.
Hydrogen
Gasoline
t = 60 sec.

## Slide 7: Metal Hydrides
Theory
Advantages
Storage performance: compact & safe
Fully Reversible
Cycling stability
Drawbacks
Operating temperature (>150°C)
Slow reaction
introduction
Absorption/Desorption Schematic
T (°C)
P (bar)
Notes: Room temperature hydrides have transitions metals, lightweight

## Slide 8: 2. Motivation

## Slide 9: Research Efforts H2 Storage
H-Mg-Ni
The Metal Hydride Center of Excellence – DOE Hydrogen Program
Identified promising lightweight elements
B - H - Li - Mg - Ni
motivation
Mg-Ni
B-Mg
H-Mg
H-Ni
Li-Mg
B-Ni
Li-Ni
H-Li
B-H
B-Li
H-Mg-Ni
B-H-Li
B-Li-Ni
B-H-Ni
B-H-Mg
B-Li-Mg
B-Mg-Ni
H-Li-Mg
H-Li-Ni
Li-Mg-Ni
Notes: Room temperature hydrides have transitions metals, lightweight

## Slide 10: Metal Hydride Investigation
Experimental investigation of metal hydrides:
    Time consuming experiments (slow kinetics)
    Sampling of full composition range
Therefore, we combined thermodynamic modeling with key experiments to investigate Mg-Ni-H system.
    Reduces experimental load
    Prediction by extrapolation
Project collaborators:
  MaSc - Guy-Joël Rocher - Experiments
  PhD - Saida Abdessameud - Thermodynamic Modelling
Motivation

## Slide 11: 3. Experimental Procedures

## Slide 12: Equipment
Planetary Ball Mill
Induction Furnace
Glove box
X-ray Diffractometer
PCT-Pro 2000
Experimental procedures

## Slide 13: Sample Preparation
Main Challenges:
Homogeneity
Oxidation
Contamination
Optimized Procedures
Sample Alloying:
Planetary Ball Milling (1hr) + Induction Melting (dissolve Ni)
Glove box:
Crushing of button sample
Load powder in test cell
Hydrogen Sorption Testing:
Volume Calibration
Activation cycles (3)
Experimental procedures
Ni 1728K
Mg 923K

## Slide 14: 4. Results and Discussion

## Slide 15
Phase Identification
Results & Discussion
Chart: 2θ Angle
XRD as cast Mg72Ni28

## Slide 16
Chart: Mass Fraction H/(Mg+Ni)
Hydrogen Sorption Testing
Results & Discussion
PCI Mg72Ni28
Mg2NiH4
MgH2
Van’t Hoff equation
Solid solution
Notes: Compare equilibrium constants, diff samples operate at diff temp & pressures

## Slide 17: Van’t Hoff Plot
Chart: 1/T (1000/K)
| 1.7452006980802792 | 1.6722408026755853 | 1.6051364365971108
MgNiH4 this work | 4.06 | 6.5 | 10.95
MgH2 this work | 1.89 | 3.38 | 6.32
Reilly Mg2NiH4 | 3.436 | 5.713 | 10.18
Buchner Mg2NiH4 | 4.03 | 6.53 | 12.06
Buchner MgH2 | 2.07 | 3.83 | 7.98
Van’t Hoff Plot Mg72Ni28
Results & Discussion
Notes: Eq. used to compare equilibrium constants

## Slide 18
Chart: Mass Fraction H/(Mg+Ni)
Phase Diagram Mg-H
PCI to Phase Diagram
Results & Discussion
PCI Mg67Ni33

## Slide 19
PCI compared to thermodynamic calculations
Results & Discussion

## Slide 20
Thermodynamic Data Mg72Ni28
Results & Discussion
Sample | Reaction | Experimental H (kJ/mol) | Calculated H (kJ/mol) | Reported H (kJ/mol) [Reilley,79]
Mg72Ni28 | Mg2NiH4 Absorption | -64.4 | - | -
 | Mg2NiH4 Desorption | -73.0 | - | -
 | Mg2NiH4 Average | -68.7 ± 5.5 | -66.4 | -64.5
 | MgH2 Absorption | -74.0 | - | -
 | MgH2 Desorption | -82.1 | - | -
 | MgH2 Average | -79.8 ± 5.5 | -78.8 | -77.4

## Slide 21: 5. Concluding Remarks & Future Work

## Slide 22: Concluding Remarks
Successful PCI experiments were carried out on the Mg-Ni-H system.
Resolved the difficulties with sample preparation.
Demonstrated effectiveness of the novel methodology
  Mg67Ni33 good agreement with literature
  Mg72Ni28 good agreement with thermodynamic calculations
Comprehensive literature review on hydrogen storage
conclusion

## Slide 23: Future Work
Complete the investigation of promising systems to find ideal candidate for commercial applications
Testing of composite samples made of metal hydrides and complex metal hydrides
2LiBH4+MgH2
Volumetric and gravimetric capacity
Good reversibility
conclusion
B - H - Li - Mg - Ni

## Slide 24: Acknowledgements
Funding H2Can Network
Dr. Huot group at UQTR (IRH)
Dr. Ottenwaelder & M. Askari access to glove box
S. Abdessameud for thermodynamic modeling

## Slide 25
THANK YOU
? ? Questions ??